## Slide 1
Phase Transitions in Soft Matter
Jamming, Glass Transition, and Rheology
Ning Xu
Department of Physics, CAS Key Laboratory of Soft Matter Chemistry & Hefei National Laboratory for Physical Sciences at the Microscale, University of Science and Technology of China

## Slide 2
Phases of matter and phase transitions
Soft Matter  Fifth?
Matter between liquids and solids

## Slide 3
Phase diagram in T-P plane
water

## Slide 4
Phase diagram in P- plane
Spinodal decomposition
metastable

## Slide 5
Phase diagram in T- plane

## Slide 6
Types of phase transitions
First order transition
Discontinuous phase transition
T, P, chemical potential  same
Entropy S discontinuous  latent heat
Second order transition (critical)
Continuous phase transition
T, P, , S same
No latent heat
Critical scaling
Order parameter  a quantity characterizing the order of a system
Take PV system as example (can be other systems)

## Slide 7
Mean field theory of phase transition
Assuming no spatial fluctuation, expanding free energy G in a power series of order parameter m (e.g. Ising model)
Appearance of cubic term  first order transition (exception: 2D Potts model)
Mean field theory works well in high dimensions
b = 0
b  0

## Slide 8
Critical scaling of critical phenomena
Phase transition happens at
Order parameter
Susceptibility
External field
Specific heat
Correlation length

## Slide 9
Characterizing critical phenomena
Scaling hypothesis
Finite size scaling
No true phase transition for finite systems with size L
Collapse curves measured at different external field in vicinity of
Collapse curves measured at different sizes in vicinity of

## Slide 10
What is Soft Matter?
Major features:
Soft
weak interactions, large response to small perturbation
Room temperature
quantum effects negligible
Complicated components, structures, dynamics, and so on
fluctuations important
Pierre-Gilles de Gennes
The Nobel Prize in Physics 1991
Polymer
Liquid crystal
Colloid
Granular material
Emulsion
Foam
Glass
Biological material

## Slide 11
Glasses
P. G. Debenedetti and F. H. Stillinger, Nature 410, 259 (2001).
Liquids are supercooled when quenched fast enough to bypass crystallization
Supercooled liquids turn into glasses (highly viscous liquids?) at low temperatures

## Slide 12
Glass transition  unusual phase transition
Liquid  disorder solid transition
No appearance of long range structural order
No latent heat  Not conventional first order transition
No apparent structural signature
No diverging two-point static length observed
 Not conventional second order transition
What type of phase transition is the glass transition?
Thermodynamic, dynamical, or not a transition at all?

## Slide 13
Characterizing structure
Radial distribution function
Probability of finding particles r distance away
Determine thermodynamic quantities:
Virial expression of pressure
Energy
Compressibility

## Slide 14
Static structure factor S(k)
S(k) and g(r) are related via Fourier transform
First peak at k = 2/a, a is about inter-particle spacing
In liquids, S(0) proportional to isothermal compressibility
Characterizing structure

## Slide 15
Two-step relaxation of supercooled liquids
Intermediate scattering function
 relaxation
 relaxation
Vogel-Fulcher function
Mode coupling function

## Slide 16
Glass fragility
Arrhenius:
Super Arrhenius:
Fragility:
Softer and denser systems are more fragile
L. Berthier and T. A. Witten, EPL 86, 10001 (2009).
J. Mattsson et al., Nature 462, 83 (2009).

## Slide 17
Dynamical heterogeneity of supercooled liquids
Non-Gaussian parameter
Four point dynamical susceptibility

## Slide 18
Aging of glasses
System is quenched to a low temperature and take measure after a waiting time
Relaxation time increases with  aging

## Slide 19
Kauzmann’s Paradox
Walter Kauzmann 1948
Entropy of liquid is lower than that of crystal below some temperature

Solution: ideal glass transition temperature

## Slide 20
Potential energy landscape
PEL sampling depends on temperature
and cooling rate

## Slide 21
Ultrastable glasses
Method: vapor deposition on a substrate maintained at a temperature T
It is claimed that the glass is comparable to glasses aged over thousands of years; low energy; ultrastable; ideal glass transition
S. Singh et al. Nature Mater. 12, 139 (2013.)

## Slide 22
Glass transition is challenging
There are more theories of the glass transition than there are theorists who propose them.
David Weitz
The deepest and most interesting unsolved problem in solid state theory is probably the theory of the nature of glass and the glass transition.
Philip Anderson
K. Chang, The nature of glass remains anything but clear, The New York Times (2008).
Free volume theory
Mode coupling theory
Thermodynamic theory
Kinetic theory
Random first order transition theory
More …

## Slide 23
Colloidal suspensions
Definition: A substance microscopically dispersed evenly throughout another one
Visible particle size (~1000nm)
Brownian motion (thermal systems)
Big size in space, slow in time, ideal experimental systems to simulate
molecular systems
Medium / Phases |  | Dispersed phase |  | 
 |  | Gas | Liquid | Solid
Dispersion medium | Gas | NONE (All gases are mutually miscible) | Liquid aerosol Examples: fog, hair sprays | Solid aerosol Examples: smoke, ice cloud, air particulates
 | Liquid | Foam Example: whipped cream, shaving cream | Emulsion Examples: milk, mayonnaise, hand cream | Sol Examples: pigmented ink, blood
 | Solid | Solid foam Examples: aerogel, styrofoam, pumice | Gel Examples: agar, gelatin, jelly | Solid sol Example: cranberry glass

## Slide 24
Excluded volume repulsion
Hard particle
Electrostatic interaction
Long-range, Debye screening
van der Waals forces
Short-range, attractive, dipole-dipole interaction
Entropic forces
Attractive depletion effect in bi-disperse systems
Steric forces
Polymer induced
Interaction of colloidal suspensions

## Slide 25
Phase diagram of hard colloids
Volume fraction (density) or entropy driven

## Slide 26
Soft colloids  PNIPAM
Poly(N-isopropyl acrylamide)
decrease temperature
increase size
lower temperature
increase density

## Slide 27
Untrasoft colloids  star polymers, charged colloids
Charged colloid
Star polymer
Reentrant crystallization and glass transition

## Slide 28
Granular materials
H.M. Jaeger et al., Rev. Mod. Phys. 68, 1259 (1996)
Athermal
For sand,
Dissipative
Static friction, inelastic collisions
Angle of repose
Maximum angle before grains flow driven by gravity
Height independent pressure
Pressure saturates after the height reaches a critical value
Contact forces, static frictions with container

## Slide 29
Heterogeneous force chains
Possible cause of anomalous energy transport, e.g. sound propagation in sand
Shear banding
Shear flow and static packing of grains coexist
Nonlinear velocity profile
Shear stress gradient
Phase separation
Grains with different sizes segregate
Brazil-nut effect, reverse Brazil-nut effect
http://www.phy.duke.edu/~bob/
http://jfi.uchicago.edu

## Slide 30
Close packing of hard spheres
Kepler’s conjecture: No arrangement of equally sized spheres filling space has a greater average density than that of the cubic close packing (face-centered cubic) and hexagonal close packing arrangements. (Almost proved by T. Hales recently)
FCC
HCP
Volume fraction: Ratio of total particle volumes to volume of container

## Slide 31
Random close packing of hard sphers
In 1960’s Bernal found experimentally that when equal-sized ball bearings
were randomly poured into a container the maximum volume fraction was
always around 64%  random close packing
In two dimensions, random close packing is around 84%
J.D. Bernal, Nature 188, 910 (1960)
‘‘The figure for the occupied volume of random close packing— 0.64—must
be mathematically determinable, although so far as we know undetermined.’’
 Bernal and Mason (1960)

## Slide 32
Possible connections between close packing and random close packing, crystallization and glass transition
Structure: Ordered Disordered
Maximum density: Close packing Random close packing
Phase transition: Crystallization Glass transition
First order (Random) first order ?
Phase separation: Liquid & crystal Liquid & glasses ?

## Slide 33
Shear induced phase transition
Lee et al., Science 323, 231 (2009)
Weitz, Science 323, 214 (2009)
Grains flow when applied shear stress is larger than yield stress
Polymer glass melts when stretched

## Slide 34
Shear rheology
Shear stress
Shear strain
Shear rate
Viscosity
Shear modulus
Complex shear modulus
Storage modulus
Loss modulus

## Slide 35
Shear thinning and shear thickening
Newtonian fluids:
shear rate/stress
viscosity
water
shear rate/stress
viscosity
Non-Newtonian fluids:
Shear thinning
Shear thickening
shear rate/stress
viscosity
cornstarch-water mixture
cornstarch swimming pool

## Slide 36
Three ways to cause non-crystalline liquid-solid transition
Temperature driven
Density driven
Shear stress driven

## Slide 37
Jamming everywhere
traffic jam
crowded people
packing of fruits
sand dunes
avalanches
shaving cream

## Slide 38
Jamming phase diagram
Liu and Nagel,
Nature 396, 21 (1998)
colloidal glass
random close packing
molecular glass
shear flow
Temperature
Shear stress
Density -1
Common features: 1. liquiddisordered solid transition
2. out of equilibrium: metastable, long relaxation times
3. viscoelastic: elastic at short time, viscous at long times
Jammed
Unjammed

## Slide 39
volume fraction

Point J
unjammed
jammed
pressure, shear modulus> 0
pressure, shear modulus = 0
c
Point J  Jamming transition of packings of
frictionless spheres
Correspond to random close packing

## Slide 40
Simulation model
x
y
z
Periodic boundary conditions
Dimension of space d
Box side length L
Polydispersity or bidisperse  avoid crystallization
N/2 large and N/2 small frictionless spheres
with diameter ratio R = L /   1
R = 1.4 is usually adopted
R = 1 (monodisperse) is good for 3D, not for 2D

## Slide 41
 = 2 : harmonic  = 5/2 : Hertzian
Spring-like repulsions
Purely repulsive interaction of jammed systems
harmonic
Hertzian

## Slide 42
Lennard-Jones model of liquids and glasses
Potential cutoff at
Lennard-Jones (LJ, attractive):
Weeks-Chandler-Andersen (WCA, repulsive):
guarantees at potential cutoff
Liquid theory: Repulsion determines properties of dense liquids
Attraction acts as perturbation

## Slide 43
Units
length :  (small particle diameter)
energy :  (interaction energy scale)
mass : m (particle mass)
time :
Boltzmann constant kB = 1

## Slide 44
Energy minimization methods
Why use it?
To quickly find local potential energy minima, i.e. solids at T = 0 with each particle force balanced
Total potential energy
Local energy minima means
Start at a point P0. As many times as needed, move from point Pi to the point Pi+1 by minimizing along the line from Pi in the direction of the local downhill gradient −∇f(Pi).
 Molecular dynamics simulation with damping force
Low efficiency!
Numerical Recipes online book
http://www.nrbook.com/a/bookfpdf.php
Steepest descent

## Slide 45
Conjugate gradient
http://www.nrbook.com/a/bookfpdf.php
L-BFGS
http://www.eecs.northwestern.edu/~nocedal/lbfgs.html
SD
CG
FIRE
E. Bitzek et al., PRL 97, 170201 (2006).

## Slide 46
Molecular simulations
Molecular dynamics simulation
Monte-Carlo simulation
Reference books
Numerically integrate equations of motion of all particles
Sample configuration space using trial moves satisfying thermodynamic laws
M. P. Allen and D. J. Tildesley, Computer simulation of liquids (Oxford Science Publications, New York, 1987).
D. Frenkel and Berend Smit, Understanding molecular simulation, from algorithms to applications (Academic Press, 2002).

## Slide 47
Historic dependence of random close packing
S. Torquato et al., PRL 84, 2064 (2000).
M. Ozawa et al. PRL 109,205701 (2012).
When jamming of hard spheres is approached by different rates, hard spheres
can jam over a range of volume fractions
Random close packing is mathematically ill-defined, which should be defined
as maximally random jammed (MRJ) state alternatively
Jamming density varies if quenching hard sphere states equilibrated at densities
higher than mode couple density

## Slide 48
Random close packing is most probable
C.S. O’Hern et al., PRE 68, 011306 (2003).
C.S. O’Hern et al., PRL 88, 075507 (2002).
N. Xu et al., PRE 71, 061306 (2005).
For finite size systems, spheres jam over a range of volume fraction, P()
P() narrows with increasing system size and approaches -function at
random close packing in thermodynamic limit

## Slide 49
Structural signatures of jamming transition
Second peak of g(r) splits
, small-small
, large-large
Liquid
Peak at splits into two sub-peaks at and
Occur as well in glass formation
Right hand side of the sub-peaks approach step function at Point J
 A structural signature of T = 0 jamming transition
N. Xu and E.S.C. Ching, Soft Matter 6, 2944 (2010).
L. E. Silbert et al., PRE 73, 041304 (2006) .

## Slide 50
L. E. Silbert et al., PRE 73, 041304 (2006).
First peak of g(r) diverges
Height of first peak
Width of first peak

## Slide 51
d
C. Zhao, K. Tian, and N. Xu, PRL 106, 125503 (2011).
Critical scaling relations of jamming
Potential energy
Pressure
Bulk modulus
Shear modulus
Coordination number
average number of interacting
neighbors per particle

## Slide 52
Marginally Jammed
d
C.S. O’Hern et al., PRE 68, 011306 (2003).
C. Zhao, K. Tian, and N. Xu, PRL 106, 125503 (2011).
Critical scaling of marginal jamming
Potential energy
Pressure
Bulk modulus
Shear modulus
Coordination number
Marginal jamming:

## Slide 53
Jamming transition at Point J has mixed continuous and discontinuous
phase transition behaviors
, while for crystal it is not a function of density
Jamming transition at Point J is isostatic:
Is there an order parameter?
If any and if jamming transition is critical, I would guess it is the
coordination number  independent of potential
Special features of jamming transition

## Slide 54
i
For d-dimensional system consisting of N frictionless
spheres, total number of unknowns (x1,y1,z1,…,xN,yN,zN)
is dN; total number of constraints is zN/2
In order to determine all freedoms,
Isostatic value is minimum requirement of stability
Jamming transition at Point J is on verge of instability
Isostaticity  Maxwell criterion

## Slide 55
jammed
almost unjammed
T.S. Majmuder et al., PRL 98, 058001 (2007)
Experimental study of marginal jamming

## Slide 56
Marginally Jammed
Deeply Jammed
d
Critical scaling of deep jamming
Potential energy
Pressure
Bulk modulus
Shear modulus
Coordination number
Do not depend on potential!
C. Zhao, K. Tian, and N. Xu, PRL 106, 125503 (2011).

## Slide 57
W. G. Ellenbroek et al. PRL 97, 258001 (2006).
Probing criticality of Point J
Response to point inflation in jammed solids
More particles show response to the point force approaching Point J from above

## Slide 58
Probing criticality of Point J
Response to drag below jamming
J. A. Drocco et al, PRL 95, 088001 (2005).
More particles response approaching jamming
with a length , to 0.7

## Slide 59
P. Olsson and S. Teitel, PRL 99, 178001 (2007).
Scaling collapse of viscosity in shear flow
Probing criticality of Point J

## Slide 60
Finite size scaling
Probing criticality of Point J
H. Liu, X. Xie, and N. Xu, to be submitted.
with

## Slide 61
If a potential energy minima is slightly perturbed by moving particles from
to , rise of potential energy is
0
Dynamical (Hessian) matrix H (dN  dN)
,: Cartesian coordinates
i,j: particle index
Diagonalization of dynamical matrix
Eigenvalues : frequency of normal mode of vibration l
Eigenvectors : polarization vectors of mode l
Normal modes of vibration (phonons)

## Slide 62
Why eigenvalues correspond to frequency of normal modes?
Fourier transform
Due to periodic boundary conditions, d out of dN modes are trivial
zero-frequency modes (identical translational moves of all particles)
Rattlers: particles with NO interactions
Each rattler contributes d trivial zero-frequency modes
If there are Nf rattlers, total number of non-trivial
normal modes is d(N  Nf  1)
A State is mechanically unstable (unjammed) if any of the
d(N  Nf  1) modes has imaginary frequency ( < 0)
Apply ARPACK to numerically diagonalize large matrices
http://www.caam.rice.edu/software/ARPACK/

## Slide 63
Density of states: number of normal modes per unit frequency
For crystals, density of states obey Debye law,
Excess anomalous low-frequency modes beyond Debye prediction form a plateau
Onset frequency of plateau shifts to zero at Point J
: speed of sound
Isostaticity determines special vibrational properties of jammed systems
L. E. Silbert et al., PRL 95, 098301 (2005).
N. Xu et al., PRL 98, 175502 (2007).
Density of vibrational states of jammed solids

## Slide 64
Boson peak and its connection to stability of disordered solids
S. Singh et al., Nature Mater. 12, 139 (2013).
D
Modes beyond Debye prediction form boson peak
Disordered solids like glasses are more stable with higher
boson peak frequency

## Slide 65
Picture of modes
low frequency
quasi-localized
intermediate frequency
extended
high frequency
localized

## Slide 66
Participation ratio of modes
Modes are more localized with smaller

## Slide 67
Connection between quasi-localization and stability of disorder solids
Along more localized low-frequency modes, energy barrier are lower
Disorder solids like glasses are more stable if low-frequency quasi-localization
is weaker
N. Xu et al., EPL 90, 56001 (2010).

## Slide 68
Why normal modes?
A. Widmer-Cooper et al., Nature Phys. 4, 711 (2008)
Structural relaxation of supercooled liquids shows strong correlation with low-frequency quasi-localization of T = 0 glasses
It is feasible to probe glass transition from the T = 0 glass perspective
Normal modes of vibration (phonons) are basic element to understand unusual properties of disordered solids, e.g. energy transport, mechanical and dynamical heterogeneity upon excitations, …
Crystal
Glass

## Slide 69
Modified jamming phase diagram
Glass transition at is at a volume fraction lower than Point J
Discontinuous change of yield stress at
A. Ikeda et al., PRL 109, 018301 (2012).

## Slide 70
Jamming of frictional spheres
Forbidden
Allowed
C. Song et al., Nature 453, 629 (2008).
Yellow region is theoretically allowed
jammed regime
D. Bi et al., Nature 480, 355 (2011).
Shear induced jamming

## Slide 71
Jamming of non-spherical particles
A. Donev et al., Science 303, 990 (2004)
Z. Zeravcic, N. Xu et al., EPL 87, 26001 (2009).
M. Mailman et al., PRL 102, 255501 (2009).
NYU P. Chaikin’s office

## Slide 72
Collective behaviors of active matter
A new field in soft matter physics.
Objects: Properties of assemblages of self-propelled particles
 converting energy to movement.
Schools of fish
Flocks of birds
Swarms of bacteria
Schools of sheep
Crowded people